# Group-14 experimental data

# Appendices

Appendix A: Observed Data

Basis: 12 g of catalyst

Ratio of Al2O3: NiO = 5:1

Mass of Catalyst used = 3 g

Table 1: Observed flowrates of different chemical species.

| Stream | Flowrate |
| --- | --- |
| N2 | 20 L/min |
| H2 | 10 L/min |
| CO | 8 L/min |
| Outlet | 550 cm3/min |

Outlet mixture flow rate, Q=7.7 cm3/min =0.462 L/h
Reaction pressure = 760 mmHg

Calcination temperature = 350 ℃

Reaction temperature = 350 ℃

Room temperature = 32 ℃

Table 2: Gas Chromatography results of Standard sample and Test sample.

| Component | Area Under the Peak (Standardized) | Calculated Molar Composition (%) | Standard Molar Composition (%) | Area Under the Peak (Sample) |
| --- | --- | --- | --- | --- |
| H2 | 39584 | 2.878 | 48.27 | 2360 |
| N2 | 566603 | 46.105 | 31.80 | 821493 |
| CH4 | 215451 | 3.394 | 8.37 | 87367 |
| CO | 133058 | 10.750 | 6.13 | 233359 |
| CO2 | 23041 | 11.045 | 1.40 | 181783 |
| Ar | 144817 | 0.297 | 1.40 | 7394 |

## Appendix B: Calculated Data

Dry gas flow rate at NTP = 17.58×10-3 molhr

Molar flow rate of outlet gas = 18.45×10-3 molhr

Required mass of Ni(NO3)2∙6H2O = 7.785 g

Required mass of Al(NO3)3∙9H2O = 73.55 g

Table 3: Molar flow rates of inlet streams.

| Component | Flow rate (mole/h) |
| --- | --- |
| N2 | 0.799 |
| H2 | 0.399 |
| CO | 0.320 |

Table 4: Gas composition of outlet stream.

| Component | Measured Composition (%) | Normalized Composition (%) | Flow rate (molhr) |
| --- | --- | --- | --- |
| H2 | 2.878 | 3.865 | 6.795×10-4 |
| N2 | 46.105 | 61.912 | 1.088×10-2 |
| CH4 | 3.394 | 4.558 | 8.013×10-4 |
| CO | 10.750 | 14.436 | 2.538×10-3 |
| CO2 | 11.045 | 14.832 | 2.607×10-3 |
| Ar | 0.297 | 0.399 | 7.014×10-5 |

Conversion of CO = 99.207%

Selectivity of CH4 with respect to CO2 = 0.307

## Appendix C: Sample Calculation

Catalyst Mass Determination

Basis: 12g of catalyst.

The ratio of Al2O3: NiO =  5 : 1

Mass of NiO in catalyst = 1 × 126=2 g

Mass of Al2O3 in catalyst =4×126=10 g

NiO is formed by the following reaction:

Ni(NO3)2.6H2O → Ni(NO3)2 + 6H2O

Ni(NO3)2 + 2KOH→ Ni(OH)2+ 2KNO3

Ni(OH)2 → NiO+H2O

1 mole NiO ≡ 1 mole Ni(NO3)2.6H2O

74.70 g NiO ≡ 290.80 g Ni(NO3)2.6H2O

The required amount of Ni(NO3)2.6H2O = 290.80×274.71=7.785 g

Al2O3 is formed by the following reaction

Al(NO3)3.9H2O → Al(NO3)3 + 9H2O

Al(NO3)3 + 3KOH→ Al(OH)3 + 3KNO3

2Al(OH)3→Al2O3+3H2O

2 mole Al(NO3)3.9H2O ≡ 1 mole Al2O3

750.26g Al(NO3)3.9H2O ≡  102g Al2O3

The required amount of Al(NO3)3.9H2O = 375.13×10×2102=73.55 g

Inlet gas flow rates

H2 =  10 Lhr×273 K×760 mm Hg×1gmole(273.15+32) K×760 mm Hg×22.4 L=0.399 gmolehr

N2 = 20 Lhr×273K×760 mm Hg×1gmole(273.15+32)  K×760 mm Hg×22.4 L=0.799 gmolehr

CO = 8 Lhr×273 K×760 mm Hg×1gmole(273.15+32)  K×760 mm Hg×22.4 L=0.320 gmolehr

Outlet gas volumetric flow rate, Vtot  =  7.7 cm3min×60min1hr×1 m3106 cm3  =462×10-6 m3hr

Molar flow rate =  ntot

We know,

PVtot= ntotRT

or,  ntot= PVtotRT   =462×10-6 × 101325×1305.15 ×8.314  =18.45×10-3 gmolehr

At 32oC, Vapor pressure of water = 35.7 mmHg (NIST WebBook)

Dry gas flow rate at NTP = ndry

Since P α n (Avogadro’s law),

∴ ndry =Pdry×ntotPtot

=18.45×10-3 gmolehr×760-35.7mmHg760 mm Hg  = 17.58×10-3 gmolehr

Outlet gas composition

H2=236039584×48.27%=2.878 %

N2 =821493566603×31.80%=46.105 %

CH4=87367215451×8.37%=3.394 %

CO=233359133058×6.13%=10.750 %

CO2=18178323041×1.40 %=11.045 %

Ar =7394144817×1.40 %=0.297 %

Total mole percentage in outlet gas without normalization = 74.469 %

Normalized mole percentage of outlet gas

H2 =2.87874.469 ×100 %=3.865 %

N2 =46.10574.469 ×100 %=61.912 %

CH4 =3.39474.469 ×100 %=4.558 %

CO =10.75074.469 ×100 %=14.436 %

CO2 =11.04574.469 ×100 %=14.832 %

Ar =0.29774.469 ×100 %=0.399 %

Outlet gas flow rate (dry basis) from GC data

H2 =17.58×10-3 ×3.865100 =6.795×10-4 mol/h

N2 =17.58×10-3 ×61.912100 =1.088×10-2 mol/h

CH4 =17.58×10-3 ×4.558100 =8.013×10-4 mol/h

CO =17.58×10-3 ×14.436100 =2.538×10-3 mol/h

CO2 =17.58×10-3 ×14.832100 =2.607×10-3 mol/h

Ar =17.58×10-3 ×0.399100 =7.014×10-5 mol/h

Conversion of CO = COin-COoutCOin×100%=0.320-2.538×10-30.320×100=99.207 %

Selectivity = Desired product formed (CH4)Undesired product formed (CO2)=8.013×10-42.607×10-3=0.307